[image: image1.wmf]Technical Data Sheet

Nazdar 720 Series UV Inkjet


	Primary uses of this product are for POP displays, durable graphics and banners where color fidelity and adhesion are of primary importance. Typical substrates for this graphic ink are: acrylics, styrene, Dibond, foam boards, Sintra, rigid and flexible vinyl, rigid PVC, pressure sensitive banner, blue-back paper, and window cling.


Primary Features & Substrates

Features

· Formulated for use in multiple applications with adhesion to a wide variety of flexible and rigid substrates.
· Excellent resistance to edge chipping on rigid substrates when used with a knife or router cutter

· Resists degradation by the most common double sided adhesives used in 2nd surface applications (3M® 467MP)

· Allows adhesion of poster glues typically used in multi-layer billboard applications
· Long term exterior performance with proven resistance to the effects of UV degradation and color fade.

· High impact, high intensity colors with extended color gamut

· Consistent color density values

· Heat Bendable
Substrates

· Acrylics

· Reinforced vinyl banner, pressure sensitive vinyl, and window cling

· Styrene

· Rigid Polyethylene
· Fluted Polypropylene

· Foamboard

· Polycarbonate

· Teslin® Synthetic Paper

· Blue Back poster paper

Adhesion should always be tested as adhesion does depend upon curing conditions, age and manufacturer of substrate. 
Ink Handling

All personnel mixing and handling this product must wear gloves and eye protection. Clean up all spills immediately. If ink does come in contact with skin, wipe ink off with a clean, dry cloth (do not use solvent or flush solution). Wash the affected area with soap and water. Consult the Nazdar® 720 Series Safety Data Sheet for further instructions and warnings.

Ink Changeover

Thoroughly clean your current ink system and jet assemblies with LWU7001FF UV Flush Solution.  Avoid contact with skin. Wear protective safety glasses and appropriate gloves when handling flush solution. Consult SDS for proper procedures for using Flush solution. Complete conversions procedures available upon request. 

When UV inkjet equipment is not in use for extended periods of time the ink should be flushed from the printheads to avoid unwanted in-head curing from stray light sources.

Curing Parameters

Nazdar® 720 Series Ink has been formulated to cure when exposed to a focused, medium pressure mercury vapor lamp providing 225 – 300 mJ/cm² and 600 mW/cm².  (EIT Uvicure Plus radiometer, measuring the UVA spectrum)

Clean Up

For clean-up of ink spills and equipment use LWU7001FF UV Maintenance Solution.
Storage/Shelf Life

Store ink and flush solutions at 18° - 27° C (65° - 80° F). Ink and flush solutions should always be kept away from heat, sparks, and flames.  If stored at a different temperature, the ink should be allowed to reach room temperature before calibration or printing.  The shelf life of this product is 12 months from the date of manufacture when stored under prescribed conditions.
Ink Performance

Outdoor Durability

When Nazdar® 720 Series Ink is used with the proper color management; color variance will be minimal over a period of 24 months vertical outdoor exposure. Outdoor durability is based on actual outdoor weather testing in the central US.

To ensure Nazdar® 720 Series Ink density and hue values do not change during outdoor exposure, it is important to use proven substrates (flexible vinyls and pressure sensitive vinyls) that do not “yellow” or vary from their original white cast when exposed outdoors.
Environmental Operating Parameters

Temperature:

· 65 ˚ F – 80 ˚ F [18 ˚ C – 27 ˚ C]

Humidity:

· Optimum: 40% - 60% (non-condensing)

· Operational: 30% - 70% (non-condensing)

Nazdar Quality Statement

Nazdar® stands behind the quality of this product.  Nazdar® cannot, however, guarantee the finished results because Nazdar® exercises no control over individual operating and production procedures.  While technical information and advice on the use of this product is provided in good faith, the user bears sole responsibility for selecting the appropriate product for their end use requirements. Users are also responsible for testing to determine that our product will perform as expected during the printed item’s entire life cycle from printing, post print processing, and shipment to end use. This product has been specially formulated for inkjet printing, and it has not been tested by any other method.  Any liability associated with the use of this product is limited to the value of the product purchased from Nazdar®.

Based on information from our raw material suppliers, these products are formulated to contain less than 0.06% lead. If exact heavy metal content is required, independent lab analysis is recommended.


Validated Equipment

Nazdar® 720 Series Ink has been validated for use in the following printer platforms:

· Durst Rho 800

· Inca Onset S-20 (w/o autoloader)

· Inca Spyder

· Agfa/Gandi Jeti 1224 UV

· HP Scitex FB6100

· NUR Tempo Q

· Jetrix 2030FRK

· Polytype Virtu RS-35

· CET Color X-Series (Polaris)
Manufacturers Product Offering

All colors listed in the table below are available in 1 and 5 liter containers. Contact your Nazdar distributor for product availability and offering.

Inks

	Item Number
	Color

	LWU720CY
	Cyan

	LWU720MA
	Magenta

	LWU720YE
	Yellow

	LWU720KK
	Black

	LWU720LC
	Light Cyan

	LWU720LM
	Light Magenta

	LWU720OR
	Orange

	LWU720YL
	Light Yellow

	LWU720KL
	Light Black

	LWU720NC
	Clear

	LWU720WH
	White

	LWU720GR
	Green

	LWU720VT
	Violet

	SPECIAL ORDER NON-STOCK COLORS

	LWU720HDCY
	High Density Cyan

	LWU720HDMA
	High Density Magenta

	LWU720HDYE
	High Density Yellow

	LWU720HDKK
	High Density Black

	LWU720HDOR
	High Density Orange


Flush

	Item Number
	Color

	LWU7001FF
	UV Maintenance Solution



Ancillary Products

Adhesion Promoters/Primers

Nazdar offers a variety of adhesion promoters that can help with difficult to adhere to substrates. The table below is a guide for selecting the correct product for your application. Please refer to our technical data sheets for the primary substrates for each ink as in many cases a primer is not needed at all.

	Substrate
	Nazdar 7020
	Nazdar 7025
	Nazdar 7030

	Styrene
	
	NA
	

	Coated Alumapanel
	NA
	
	NA

	Fluted Polypropylene
	
	
	NA

	Acrylic
	
	
	

	Lexan
	
	
	

	Glass
	
	
	NA


Overprint Clears

	The following Nazdar® screen print clear products have been approved for use with the 720 Series Ink.
Item Number
	Color

	1827
	1827 Overprint Clear

	1927
	1927 Overprint Clear

	2326
	2626 Mixing Clear

	2727
	2727 Overprint Clear

	223900RP
	2-Part Urethane Clear

	3227
	3227 Overprint Clear

	4029*
	4029 Premium OP Clear*

	NSC64
	NSC64 OP Clear

	PSLC294
	PSLC294 UV Litho Clear (indoor applications only)


*Nazdar 4029 Premium Overprint Clear has shown to be the superior choice for protecting the 720 Series inks. Accelerated weather testing in a Xenon weathering chamber showed excellent results up to 2500 hours.


Backing Screen Print White

The following Nazdar® screen print white ink products have been approved for use with 720 Series Inkjet ink.
	Item Number
	Color

	1875
	1875 Super Opaque White

	1878
	1878 High Intensity White

	1950
	1950 Barrier White

	1975
	1975 Super Opaque White

	1978
	1978 High Intensity White

	2378
	2378 High Intensity White

	2775
	2775 Super Opaque White

	3478 w/catalyst
	3478 with 5% NB80

	4050
	4050 Barrier White

	4075
	4075 Super Opaque White

	4078
	4078 High Intensity White


Nazdar Ink Technologies 
Offices Worldwide

Nazdar Ink Technologies -World Headquarters
8501 Hedge Lane Terrace
Shawnee, KS 66227-3290 USA
Toll Free US:  866-340-3579
Tel: +1 913-422-1888 
Fax: +1 913-422-2296
E-mail: custserv@nazdar.com
Technical Support E-mail:  InkAnswers@Nazdar.com
Nazdar Limited – EMEA
Battersea Road, Heaton Mersey
Stockport, England SK4 3EE
Tel: + 44 (0)-161-442-2111
Fax: + 44 (0)-161-442-2001
EMEA Technical Service E-mail: technicalservicesuk@nazdar.com
Nazdar – China
Room 17-04, Silver Centre
1388, North Shan Xi Road
Shanghai 200060 China
Tel: +86-13818301261
E-mail: aspac@nazdar.com
Nazdar – Asia Pacific
11, Changi North Street 1 #03-03/04
Singapore 498823
Tel: +65-6385 4611
E-mail: aspac@nazdar.com









Page 1 of 3
© Nazdar Ink Technologies  |  www.nazdar.com   |   custserv@nazdar.com  |  InkAnswers@nazdar.com

